TECHNICAL DESCRIPTION

(LAMINATED-GLASS WINDSCREENS)

| Approval No | E4*43R01/12*2285*05 |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Information folder number: |  |  |  |  |  | 20250409 |  |
| Class of safety-glass pane |  |  | : |  | Ordinary laminated-glass windscreen |  |  |
| Description of glass pane |  |  | : |  | Please refer to Appendix 3 of ECE R43 |  |  |
| Trade name |  |  | : |  | SYP;;;; PILKINGTON; YES GLASS; |  |  |
| Name and address of manufacturer |  |  | : |  | SYP KangQiao Autoglass Co., Ltd. No.55, Kangliu, Pudong District, 201315, SHANGHAI, China (PRC) |  |  |
| Principal characteristics |  |  |  |  |  |  |  |
| Number of layers of glass |  |  | : |  | 2 |  |  |
| Number of layers of interlayer |  |  | : |  | 1 |  |  |
| Nominal thickness of the windscreen |  |  | : |  | 4.96 mm |  |  |
| Nominal thickness of interlayer(s) |  |  | : |  | 0.76 mm |  |  |
| Special treatment of glass |  |  | : |  | No |  |  |
| Nature and type of interlayer(s) |  |  | : |  | Acoustic PVB |  |  |
| Nature and type of plastics coating(s) |  |  | : |  | not applicable |  |  |
| Nominal thickness of plastic coating(s) |  |  | : |  | not applicable |  |  |
| Secondary characteristics |  |  |  |  |  |  |  |
| Nature of the material (plate, float, sheet glass) |  |  | : |  | Float |  |  |
| Colouring of glass (colourless/tinted) |  |  | : |  | colourless/tinted |  |  |
| Colouring of plastics coating(s) |  |  | : |  | not applicable |  |  |
| Colouring of interlayer (total/partial) |  |  | : |  | (total / partial) tinted / colourless |  |  |
| Conductors incorporated (yes/no) |  |  | : |  | yes/no |  |  |
| Opaque obscuration incorporated (yes/no) |  |  | : |  | yes/no |  |  |
| Remarks |  |  | : |  |  |  |  |

_____________________________________________________________________________

Documents attached: list of windscreens (see appendix 13).

Annex 1 - Appendix 13

CONTENTS OF THE LIST OF WINDSCREENS1/

| Information folder number: |  |  | 20250409 |
| --- | --- | --- | --- |
| For each of the windscreens covered by this approval, at least the following particulars shall be provided: |  |  |  |
| Vehicle manufacturer | : | Changan Ford Automobile Co., Ltd. |  |
| Type of vehicle | : | CX483N |  |
| Vehicle category | : | M1 |  |
| Developed area (F) | : | 1.47 m2 |  |
| Height of segment (h) | : | 105 mm |  |
| Curvature (r) | : | 992 mm |  |
| Installation angle (α) | : | 60.9° |  |
| Seat-back angle (β) | : | 22° |  |
| R-point coordinates (A, B, C) relative to the centre of the upper edge of the windscreen. | : | A: 395.4 mm B: ±375mm C: 850.6 mm |  |
| Description of the commercially available specific device mentioned in annex 3, paragraph 4.9.2. (if applicable) | : | not applicable |  |